Construction Specification

Section 02825 –Architectural Metal Fenceworks Inc.

Palisade High Security Steel Perimeter Fence System

- General

  - Included Work:

These specifications include Palisade security fence, gates, posts and hardware. Contractor is to provide labor and concrete.

  - Related Work:

Section		Earthwork

Section		Concrete

Section		Painting

  - System Description:

Manufacturer shall supply a complete fencing system including posts, rails, pickets, fish plates, mid bay supports, gates and hardware.

  - Quality Assurance:

Contractor shall supply laborers and supervisors who are familiar with Palisade security fence installation and	construction.

  - References:

ASTM A036		Structural Steel

ASTM A500		Cold Formed Steel

ASTM A513		Low Carbon Steel

ASTM B117-90		Salt Spray Resistance

ASTM D3363		Gouge Pencil Hardness

ASTM D4752		MEK Test – 50 Double Rubs

ASTM D3359		Adhesion

ASTM D522-93A		Elongation

ASTM D2794		Impact Resistance Min. 140 inch lbs

ASTMG007		South Florida Exposure

  - Submittal:

Manufacturers shop drawings, literature and installation procedures shall be submitted to 	insure compliance with 	requirements for materials specified.

  - Product:

Delivery, handling and storage all materials shall be inspected to ensure that no damages were incurred during shipping. 	Materials are to be stored in a clean, dry, dust and chemical free environment and in an area where materials will be secure from 	vandalism and theft.

- Products

  - Manufacturer:

The PalisadeFence™ steel fence system shall be manufactured by:

Ironworks Mfg. & Supply Co.

300 W. South Street

Jackson MS  39203

877-379-8305 or 601-352-3722

  - Materials:

- All solids, pales, posts, angles, channels, and I-beams will be made from steel with requirements of ASTM A36.

- Pales on gates shall be the same size and specifications as fence. Gate frames will meet requirements of ASTM A500 grade B or ASTM 513.

- All steel components shall be hot dip galvanized to ASTM 123 and will be a minimum of 3.5mils thick inside and outside of all steel components.

- All steel components shall be coated with a minimum of 2.5 mils of TGIC polyester powder coat.

  - Fabrication:

- All steel used in manufacturing of fencing will be of new clean steel conforming to ASTM requirements.

- Pales are fastened to the rails with security fastenings to form the panel. The fence panels are fastened to other fence panels through the posts using fish clips with security fasteners.

- Swing gates shall be using pales used in fence.  All connections and intersections shall be welded prior to hot dip galvanize and powder coating.

- Completed fence panels shall be able to support 500 lb. load applied at center of fence panel without permanent damage.

- Panels shall have an adjustable pitch of 0° to 15°.

- Execution

  - Preparation:

- Contractor shall layout new fence according to fence construction plans, shop drawings and codes or applicable requirements.

- Contractor shall check for grade changes.

- All discrepancies between plans, shop drawings and site conditions must be approved by architect or engineer before proceeding further.

(Continued on page 2)

Construction Specification

Section 02825 –Architectural Metal Fenceworks Inc.

Palisade High Security Steel Perimeter Fence System

Page 2

  - Installation:

- Posts will be set at a maximum of 9’-0” on center having footings of 12” in diameter and 3’-0” deep below finish grade (this depends on height of fence & soil conditions).

- Insert appropriate fish plates into the slots in the posts.

- Attach rails to the fish plates using appropriate bolts & security nuts.

- Install mid bay support to bottom rail.

- Attach pickets to the rails with appropriate bolts & security nuts.

- Adjust mid bay support when concrete is set.

- All abrasions to factory coatings shall be free of oil, dirt rust and wax and shall be primed with cold galvanize spray and touched up with paint that matches quality, color and sheen of gloss as that of manufacturers paint.

  - Cleaning:													   	Contractor shall remove debris caused by excavation of post footings. Excess mortar concrete, strings, stakes etc. All 			posts shall have concrete splatter removed.